Sarah Heilshorn

Associate Professor

Materials Science and Engineering

Stanford University

Protein-Engineered Materials for Regenerative Medicine

Stem cell transplantation is a promising therapy for a myriad of debilitating diseases and injuries; however, current delivery protocols are inadequate. Transplantation by direct injection, which is clinically preferred for its minimal invasiveness, commonly results in less than 5% cell viability, greatly inhibiting clinical outcomes. We demonstrate that mechanical membrane disruption results in significant acute loss of viability at clinically relevant injection rates. As a strategy to protect cells from these damaging forces, we show that cell encapsulation within hydrogels can significantly improve transplanted cell viability. Building on these fundamental studies, we have designed a family of injectable, bioresorbable, customizable hydrogels using protein-engineering technology. By integrating protein science methodologies with simple polymer physics models, we manipulate the polypeptide chain interactions and demonstrate the direct ability to tune the material properties including hydrogel mechanics, cell-adhesion, and biodegradation. Through a series of in vitro studies, we demonstrate that material degradability is a critical requirement to maintain the "stemness" of neural progenitor cells in 3D hydrogels and that this effect is independent of mechanosensing through cytoskeletal contractility. Together, these data demonstrate that protein-engineered hydrogels may significantly improve transplanted stem cell retention and regenerative function.